## Slide 1: Tracking Oxidation in “High-Entropy” Alloys with Multiple Principal Elements
B. Gwalani, A. Martin, E. Kautz, B. Guo, S.V. Lambeets, M. Olszta, A.K. Battu, A. Malakar, F. Yang, J.-H. Guo, T. Suntharampillai, R. Li, A. Amassian, M. Thuo, and A. Devaraj, Nat. Commun. 15, 5026 (2024), doi:10.1038/s41467-024-49243-8. Work was performed at ALS/LBNL, NSLS-II/BNL, and PNNL.
Scientific Achievement
Researchers learned how the various elements in a complex ("high-entropy") alloy contribute to oxidation at high temperatures.
Significance and Impact
The work will inform both the development of future alloys and how we can use those alloys in real-world applications.
Progression in speciation during oxidation of a five-component high-entropy alloy (CoCrFeNiMn, also called the Cantor alloy). The panels show the elemental distribution during initial oxidation at t = 0 (left), 0 < t < ∞ (center), and t ~ ∞ (right).
Research Details
  X-ray absorption near-edge structure (XANES) measurements at the Advanced Light Source captured interactions between the elements. Other analyses included atom probe tomography at Pacific Northwest National Laboratory and grazing-incidence wide-angle x-ray scattering at National Synchrotron Light Source II.
  Overall experimental results were consistent with a thermodynamical model (Preferential Interactivity Parameter) developed by colleagues at North Carolina State University.
Notes: For extreme applications such as nuclear fusion reactors and high-temperature jet engines, scientists are experimenting with “high-entropy” alloys that consist of many metals mixed together in equal proportions. In this work, researchers have begun to unravel how these materials degrade under high-temperature oxidative environments. The researchers studied a high-entropy alloy with equal amounts of the metals cobalt, chromium, iron, nickel, and manganese (CoCrFeNiMn, also called the Cantor alloy). They used a variety of methods, including grazing-incidence wide-angle x-ray scattering (GIWAXS) at the National Synchrotron Light Source II (NSLS-II) and x-ray absorption near-edge structure (XANES) at the Advanced Light Source (ALS).
Researchers: B. Gwalani, A. Martin, B. Guo, A. Malakar, A. Amassian, and M. Thuo (North Carolina State University); E. Kautz, S.V. Lambeets, M. Olszta, A.K. Battu, T. Suntharampilla, and A. Devaraj (Pacific Northwest National Laboratory); F. Yang and J.-H. Guo (ALS); and R. Li (NSLS-II).
Acknowledgment from paper: US Department of Energy, Office of Science, Basic Energy Sciences program (DOE BES) and Office of Naval Research. Operation of the ALS and NSLS-II is supported by DOE BES.
Full highlight: https://als.lbl.gov/tracking-oxidation-in-high-entropy-alloys-with-multiple-principal-elements/