## Slide 1: Energy-Saving, Acid-Free, Hard-Rock Lithium Extraction
S. Wang, N. Szymanski, Y. Fei, W. Dong, J.N. Christensen, Y. Zeng, M. Whittaker, and G. Ceder, Inorg. Chem. 63, 13576 (2024), doi:10.1021/acs.inorgchem.4c01722. Work was performed at ALS/LBNL.
Scientific Achievement
In situ x-ray diffraction helped researchers to develop an optimized synthesis procedure to produce Li2CO3 directly from spodumene, an abundant Li-bearing mineral, without requiring the use of acid leaching.
Significance and Impact
The approach is performed at a moderate temperature (750 °C) and uses acid-free separation. It will support the sustainable scaling of lithium production to meet growing market needs.
Left: XRD intensities from α-spodumene with Na2CO3 during heating (up to 800 °C). Right: Weight fraction of each phase as a function of temperature. The reaction of α-spodumene with Na2CO3 produces a mixture of NaAlSiO4 and Li2SiO3, with Li2CO3 anticipated as a potential product.
Research Details
  In situ x-ray diffraction (XRD) at the Advanced Light Source (ALS) enabled real-time monitoring of the reaction of sodium carbonate (Na2CO3) introduced directly to α-spodumene and its reaction products.
  The data showed that some Li+ was trapped in an inactive phase; allowed researchers to identify a suitable additive to avoid this, enabling a 90.4% lithium recovery rate using a low-cost washing procedure without acid.
Notes: The increasing popularity of hybrid and electric vehicles is driving a surge in global lithium demand, necessitating a robust and reliable supply. Currently, most lithium-ion battery cathodes are synthesized from lithium carbonate (Li2CO3) or lithium hydroxide (LiOH), both of which can be obtained by processing brines or hard rocks. While brine extraction is common, the processing of hard rocks—particularly spodumene (LiAlSi2O6)—is faster and typically yields a higher recovery rate. Lithium extraction from spodumene involves first transforming α-spodumene (the naturally occurring form) into β-spodumene (a high-temperature polymorph) through calcination (heating above 1000 °C). Then, the mineral is acid roasted (heated in strong acid) before undergoing neutralization to precipitate Li2CO3. These processes are both energy intensive and costly, posing significant sustainability and economic challenges. To develop an energy-saving, acid-free route, the researchers explored direct lithium extraction from α-spodumene through solid-state reactions.
Researchers: S. Wang, N.J. Szymanski, Y. Fei, M. Whittaker, and G. Ceder (UC Berkeley and Berkeley Lab); W. Dong and J.N. Christensen (Berkeley Lab); and Yan Zeng (Berkeley Lab and Florida State University).
Acknowledgment from paper: US Department of Energy, Office of Science, Basic Energy Sciences program (DOE BES), MINES project; Jane Lewis Fellowship (UC Berkeley). Operation of the ALS is supported by DOE BES.
Full highlight: https://als.lbl.gov/energy-saving-acid-free-hard-rock-lithium-extraction/